## Slide 1: Innovation in Concrete
Steve Waalkes, P.E.
Director of Engineering – W. Mich.
Michigan Concrete Association

## Slide 2: High Level Overview of Concrete Innovation
Competition & communication are the keys to innovation
Always lessons to learn – have to keep trying, implementing new ideas
Solving problems & making improvements before they become problems

## Slide 3: Long History of Innovation in Michigan
1909 – U.S. first full mile of concrete highway, on Woodward Ave., 6 Mile Rd. to 7 Mile Rd.
1911 – U.S. first painted centerline
1912 – U.S. first highway materials testing lab
1918 – U.S. first 4-way red/yellow/green signal
1929 – U.S. first paved runways at Ford Airport in Dearborn
1955 – World’s first freeway-to-freeway interchange
1960 – U.S. first state to complete border-to-border interstate (I-94, Detroit to New Buffalo)

## Slide 4: Recent History of Concrete Innovation in Michigan
Movement towards Performance Related Specifications
Midwest Concrete Consortium started (precursor to NC2) – state DOT’s and industry collaboration
Increase in state gas tax funding; included are requirements for pavement warranties and LCCA
P1Mod spec first developed by MDOT concrete engineers
Re-tooling of the P1Mod spec; requires 3 aggregates, well-graded, optimized blend
Mid-1990’s
1997
2004

## Slide 5: Recent History of Concrete Innovation in Michigan (cont.)
P1Mod upgraded: stockpile management, process control
MCA funded study indicates ASR, air entrainment, and other issues are to blame for some early durability problems
I-96 and Ambassador Gateway projects utilize stabilized subgrades
Supplementary cementitious materials required at min. of 25%
Optimized mixtures for use in bridge elements
FHWA, CP Tech Center, and MDOT start NC2 PEM implementation
2005
2006
2010
2015

## Slide 6: Recent History of Concrete Innovation in Michigan (cont.)
MDOT specs allow ASTM C595 Type IL cement
MDOT demonstrates 30- and 50-year designs, utilizing stabilized subgrades (among other improvements)
WisDOT adopts optimized/well-graded concrete mixtures
New MDOT spec book, P1M now called 3500HP
MCA & MDOT discussing innovative concepts including:
  Stabilized subgrades; Thickened edge for truck lane; Recycling concrete into 3-inch minus material, into subgrade
2015
2018
2020
2021

## Slide 7: FHWA Emphasis on Pavement Foundation(s)
“…ME designs do not consider the effects of any deterioration or spatial variability in the foundation layers. Over time, the conditions of the foundation layers can degrade and deform under the influence of repeated heavy loads, leading to non-uniform support conditions and localized failures. Thus, the principal role of a robust pavement foundation is ensuring the foundation layers retain their integrity throughout the pavement life.”

## Slide 8: MDOT Specifications:
12SP-604B-11 (Quality Control and Acceptance of Portland Cement Concrete):
  Required for all trunkline
  12SP-604B
  Moving to new spec. book
3.09 Optimized Aggregate Gradation
  MDOT MQAP Manual

## Slide 9: Maximum Cement Content and W/C:
Maximum Cement Content:
  Pavements: 564 lbs.(6 sack)
  Bridge Decks: 611 lbs. (6.5 sack)
Maximum W/C Ratio:
  0.45
Benefits:
  Reduced paste content
  Reduced costs associated with cement
Difficulties:
  Dependent on Water Reducing Admixtures
    Local Cement testing

## Slide 10: Supplementary Cementitious Materials:
Improvements:
  Permeability
  Resistance to Freeze-thaw damage
  Consistency
Difficulties:
  Initial pushback/learning curve
  Can cause air issues
  Slower initial strength gains
Replacement rates:
  25%-40% replacement of Portland cement
    Replacement amount is determined by the Contractor
  40% total replacement

## Slide 11: Optimized Aggregates:
Improvements:
  Slump/Consistency
  Permeability
  Additional aggregates gradation used
Difficulties:
  Agency and Contractor understanding
    MDOT Optimized Aggregate Spreadsheet
  Ready Mix with limited bins
    Preblended aggregates
    2 aggregate gradation blends

## Slide 12: PEM (Performance Engineered Mixtures)
Pooled Fund Study
19 state DOT’s
4 national industry associations
Implement newer technologies to deliver enhanced concrete durability & maximize pavement performance

## Slide 13: PEM (Performance Engineered Mixtures)
V-Kelly Ball (V-Kelly)
Box Test
Maturity Method
Formation Factor
Surface Resistivity
Bulk Resistivity
Sequential Air Metric Apparatus/Super Air Meter (SAM)

## Slide 14: PEM Testing
V-Kelly Ball (V-Kelly):
  Has been used in the lab
  Have not required its use on Projects
  QC Test

## Slide 15: PEM Testing
Box Test:
  Has been used in the lab
  Have not required its use on Projects
  Perhaps require its use for trial batches in the future
  QC Test

## Slide 16: PEM Testing
Maturity Method:
  MDOT Special Provision
    Contractor’s option
    Open to traffic only
  Training is key:
    Fingerprints correct
  Doesn’t measure strength development – it predicts it

## Slide 17: PEM Testing
Formation Factor:
  MDOT has not used the formation factor
  Mainly focused on resistivity testing

## Slide 18: PEM Testing
Surface Resistivity:
  Testing was performed on 2 long-life (30 and 50 year) pavement projects
  Was being conducted on all freeze-thaw samples
    40+ sets of coarse aggregate samples were tested
    All testing and mix ingredients were provided to Jason Weiss at Oregon State University
  MDOT’s experience:
    Fairly high level of variability
      Must hold Probes perpendicular to the surface
      Ensure the Probes’ reservoirs are full
      Keep Probes away from voids and aggregate located on the surface
  Currently, MDOT has transitioned to Bulk Resistivity

## Slide 19: PEM Testing
Bulk Resistivity:
  Used on multiple research & pilot projects
  MDOT’s experience:
    Simpler test than surface resistivity
    Consistent results
    Ensure the sponges remain wet
    Keep away from metal
    Correlates with surface resistivity
    Correlated well with RCP in recent research project

## Slide 20: PEM Testing
Bulk Resistivity:
  Currently MDOT is collecting data
  Performed on all freeze-thaw samples
  Perhaps require its use for trial batches in the future?

## Slide 21: PEM Testing
Super Air Meter (SAM):
  MDOT owns 19 SAMs
  Introduced to Region personnel
  Pilot field Testing/Shadow SP:
    12CF601
    Requires testing for information only:
      Mainline Pavement
      Structures
      Barrier
    One test per sublot
      Typically 5 tests per day for mainline paving

## Slide 22: PEM Testing
Super Air Meter (SAM):
  Michigan Concrete Association’s SAM Certification Class:
    2 train-the-trainer classes completed
    3 certification classes completed
    In-field, on-site training in 2020

## Slide 23: PEM Testing
Super Air Meter (SAM):
  Shadow SP: 12CF601
    Placed in multiple projects:
      Previous:
        I-75, Monroe
        US-131, Grand Rapids (Rockford)
        I-69, Flint
    Information provided to Federal Highway and CP Tech Center

## Slide 24: PEM Testing
Super Air Meter (SAM):
  Shadow SP: 12CF601
    Project Complete in 2020:
      I-496, Lansing
      66 complete samples
    2021 Research Project:
      University of Michigan
      Hardened air analysis of 75 samples
    Future projects?
Lansing

## Slide 25: PEM Testing
Super Air Meter (SAM):
  MDOT’s Experience:
    Introduce the SAM gauge
    Inspectors experience
    Time to run the test
    Do not store wet gauges in cases
    Do not leave the gauges in the air-conditioned cab prior to testing
    Always have spare batteries
    Have a backup gauge
    Use the Shotgun
    Follow the gauge’s directions

## Slide 26: PEM Testing
Super Air Meter (SAM):
  Future Use:
    QC?
    Mix Design Verification?
    Quality Assurance Daily Test?
    Random number Testing?
    PWL?

## Slide 27: Summary
Michigan has a history of innovation
More innovation in the works
Not all innovations prove themselves to be worth it
Concrete open and suited to innovation
We have the tools to properly assess Performance Related Specifications and new materials to be added to concrete

## Slide 28: Special Thanks To:
Ethan Bahmer, MDOT CFS Bahmert1@Michigan.gov (517) 230-0190